## Slide 1
Strategy for runaway emulation
TFPIX Cornell U. team

## Slide 2
Strategy for runaway emulation
Specific goal
Measure the difference between the heater temperature (Th) and coolant temperature (Tc)
as a function of the coolant temperature, i.e.
Th-Tc vs Tc
Heater
TIM
Carbon Fiber/foam
Tc
Coolant
Flow
Glycol
Theater
Power supply
Use Moresco PPE
General set up
Feedback loop
Thermocouple

## Slide 3
Unit cell sample (ucs)
Neighbor mod.
“One module space-region”
Dimensions according to location of Neighbor modules, Cooling circuit.
Gluing according to single tube testing

## Slide 4
Single tube sample view
Carbon Fiber(CF)
Carbon Foam(Cf)
Adhesive
Half 1(h1)
Tube
Half 2(h2)
Adhesive: Hysol EA 9396 (Phase I BPix), CVD loaded, Graphite loaded, others.
Tubing: Stainless steel => OD=3mm, ID 2.5 mm

## Slide 5
Sample preparation
Vacuum -> aiming for uniform pressure on the heater and uniformity of the TIM layer
Red clip-> hold in place the heater. Minimal pressure

## Slide 6
Thermal runaway(TRA) simulation
sensor volume
Fluence
Value | Parameter
2.1*1016 neq/cm2 | Fluence
h=4.4 cm | length of the sensor
l=1.8 cm | width of the sensor
dd=100*10-4 cm | depletion depth
Vb=800 V | bias voltage
To=293 C | Tref
Ta=7000 C | TA
for simulation
Shift by +53 C

## Slide 7
TRA data taking- setup
Coldbox
IR camera
Glycol Bath
Power supply
multimeter
Webcam
LabVIEW
To power supply
To cooling
loop
Thermocouple

## Slide 8
TRA data taking-procedure
  Set coolant temperature Tc
  Set P=0 W, wait 3 min. then read Th (which should be = Tc).
  Initiate the feedback loop to control power supply:
  Wait 3 minutes. Then read device temperature Th.
  Next iteration: Raise power level to P(Th). Th will increase...
  Continue iterating until temperature plateaus …or thermal runaway occurs
  Reminder: testing is done at 20 degC < T < 110 degC while the effects we are trying to simulate actually will take place at around -30 degC. (the 53 degC shift would be reversed ).
Fixme

## Slide 9
TRA data taking- Th vs Tc
Increasing Tc would induce TRA* ; we are interested maximum change in temperature, i.e.
- Tc
* Increase in fluence and/or TIM performance will also induce TRA but we concentrate in one effect at a time.
TRA: Thmax-Tc = infinity
If no TRA then Thmax= Tplateau

## Slide 10
TRA: DT vs Tc
Note the Tc scale was shifted back to low temperature range.
Error bars corresponds to an estimate of 1 degC

## Slide 11
TRA Lab simulation vs Ansys
We are interested in the Ansys thermal simulation of our sample
Ansys

## Slide 12
Sample features and schematic I

## Slide 13
Sample features and schematic II